# Introduction

This test program intends to demonstrate the seal performance under site conditions after several reports of failure and inconsistency of leakage.

The subject of this testing is mechanical seal order 950969 modified. This version of mechanical seal was designed based on new seal faces geometry to include lasered wavy face technology.

# Test N°2 – (Sep 01 – Sep 07, 2023)

Second test is a duplicate of test N001, this test will be performed with same faces from test 01 without lapping or re-conditioning.

Barrier fluid will be simulated as per site conditions MonoEthylene Glycol + Water (30%/70%).

## Seal Configuration

| Seal faces |  |  |  |
| --- | --- | --- | --- |
|  | Part Drawing | Material | Face condition |
| Sleeve (1) | C0619166NL | Alloy C-276 | From Test 01 |
| Inner Seal Stator (14) | C0618722SL | Silicon Carbide (SL) | From Test 01 |
| Inner Seal Rotor (15) | C0619339SL | Silicon Carbide (SL) | From Test 01 |
| Outer Seal Stator (14.1) | C0618722SL | Silicon Carbide (SL) | From Test 01 |
| Outer Seal Rotor (15.1) | C0618723SL | Silicon Carbide (SL) | From Test 01 |

Cross Section of The New Parts

## Test Conditions & Results

|  | Job seal barrier |
| --- | --- |
| Duration | Minimum 144 |
| Speed | 2950 rpm |
| Fluid | Glycol 30/ Water 70 |
| Pressure | 70 barg |
| Inlet temp. | 40 °C |
| Outlet temp. | 43 °C |
| Inner Seal Leakage | Avg. 16.5 ml/h |
| Outer Seal Leakage | Avg. 17 ml/h |
| Flow | 13.2-12.2 l/min |

Tester Drawing D0571813

Tester unit B

Logged Data

The first 24h showed stable performance, however, barrier temperature was too low reason for reducing the cooling water flow to have higher barrier temperature.

Leakage was steady during the whole testing period.

## Manually Logged Data

## Measurements Results

| Leakage rate |  |  |
| --- | --- | --- |
|  | Inner Seal | Outer Seal |
| Total Run time [h] | 145.3 | 145.3 |
| Total Seal Leakage [ml] | 2378 | 2478 |
| Seal Leakage Rate [ml/h] | 16.5 | 17 |

## Post-Test Pictures

| IB Rotor | IB Stator |
| --- | --- |
| Ra | Ra |

| OB Rotor | OB Stator |
| --- | --- |
| Ra | Ra |

## Test Conclusion

The second test results showed very stable seal performance using Ethylene Glycol and water mixture, the leakage was low and within acceptable limits.

Seal faces didn’t show any damage or deterioration for the duration of the test exceeding 144h. This conclude that seal faces are suitable for Ethylene glycol and 70barg.